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	PRODUCT SPECIFICATION
Rubber flexible cable
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CABLE & WIRE FOR ELECTRICAL, ELV AND INDUSTRIAL PROJECTS
H01N2-D Welding Cable
Exact model: H01N2-D
PRODUCT IMAGES
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	H01N2-D · Primary



PRODUCT OVERVIEW
NexPro H01N2-D Welding Cable is supplied as a configurable rubber flexible cable product family. Catalog models are preserved exactly as H01N2-D. Use the source-derived tables below to select the required conductor construction, core arrangement, cross-section and dimensions.
	Product line
	Cable & Wire for Electrical, ELV and Industrial Projects

	Series / family
	Rubber flexible cable

	Exact model
	H01N2-D

	Applications
	Industrial equipment, Mobile machinery, Demanding flexible installations


MODEL IDENTIFICATION
	Exact model
	Product / variant
	Cable category
	Catalog model
	Configuration

	H01N2-D
	H01N2-D Welding Cable
	Rubber flexible cable
	H01N2-D
	Select from source table


TECHNICAL SPECIFICATIONS
	Parameter
	Specification

	Cable category
	Rubber flexible cable

	Catalog model
	H01N2-D

	Configuration
	Select from source table

	Manufacturer models
	H01N2-D

	10
	Nom. Insulation Thickness
(mm): 2 | Nom. outer diam. (mm): 9 | Max. Resistance of Conductor @ 20°C (Ω/Km): 1.91 | Approx.weight (kg/km): 165

	16
	Nom. Insulation Thickness
(mm): 2 | Nom. outer diam. (mm): 10 | Max. Resistance of Conductor @ 20°C (Ω/Km): 1.21 | Approx.weight (kg/km): 202

	25
	Nom. Insulation Thickness
(mm): 2 | Nom. outer diam. (mm): 11.5 | Max. Resistance of Conductor @ 20°C (Ω/Km): 0.78 | Approx.weight (kg/km): 299

	35
	Nom. Insulation Thickness
(mm): 2 | Nom. outer diam. (mm): 12.5 | Max. Resistance of Conductor @ 20°C (Ω/Km): 0.554 | Approx.weight (kg/km): 395

	50
	Nom. Insulation Thickness
(mm): 2.2 | Nom. outer diam. (mm): 14.5 | Max. Resistance of Conductor @ 20°C (Ω/Km): 0.386 | Approx.weight (kg/km): 540

	70
	Nom. Insulation Thickness
(mm): 2.4 | Nom. outer diam. (mm): 16.5 | Max. Resistance of Conductor @ 20°C (Ω/Km): 0.272 | Approx.weight (kg/km): 752

	95
	Nom. Insulation Thickness
(mm): 2.6 | Nom. outer diam. (mm): 18.5 | Max. Resistance of Conductor @ 20°C (Ω/Km): 0.206 | Approx.weight (kg/km): 988

	120
	Nom. Insulation Thickness
(mm): 2.8 | Nom. outer diam. (mm): 20.5 | Max. Resistance of Conductor @ 20°C (Ω/Km): 0.161 | Approx.weight (kg/km): 1227


ENGINEERING TABLES
H01N2-D · Source Specification Table 1
	Cross section (mm²)
	Nom. Insulation Thickness (mm)
	Nom. outer diam. (mm)
	Max. Resistance of Conductor @ 20°C (Ω/Km)
	Approx.weight (kg/km)

	10
	2
	9
	1.91
	165

	16
	2
	10
	1.21
	202

	25
	2
	11.5
	0.78
	299

	35
	2
	12.5
	0.554
	395

	50
	2.2
	14.5
	0.386
	540

	70
	2.4
	16.5
	0.272
	752

	95
	2.6
	18.5
	0.206
	988

	120
	2.8
	20.5
	0.161
	1227

	150
	3
	23
	0.129
	1529
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