CABLE & WIRE FOR ELECTRICAL, ELV AND INDUSTRIAL PROJECTS

# H05V-K Flexible PVC Insulated Wire

Exact model: H05V-K

PRODUCT IMAGES

| H05V-K · Primary | H05V-K · Gallery |
| --- | --- |

PRODUCT OVERVIEW

NexPro H05V-K Flexible PVC Insulated Wire is supplied as a configurable single-core flexible wire product family. Catalog models are preserved exactly as H05V-K. Use the source-derived tables below to select the required conductor construction, core arrangement, cross-section and dimensions.

| Product line | Cable & Wire for Electrical, ELV and Industrial Projects |
| --- | --- |
| Series / family | Single-core flexible wire |
| Exact model | H05V-K |
| Applications | Equipment connections, Flexible wiring, OEM electrical assemblies |

MODEL IDENTIFICATION

| Exact model | Product / variant | Cable category | Catalog model | Configuration |
| --- | --- | --- | --- | --- |
| H05V-K | H05V-K Flexible PVC Insulated Wire | Single-core flexible wire | H05V-K | Select from source table |

TECHNICAL SPECIFICATIONS

| Parameter | Specification |
| --- | --- |
| Cable category | Single-core flexible wire |
| Catalog model | H05V-K |
| Configuration | Select from source table |
| Manufacturer models | H05V-K |
| 1x0,5 | Resistance at 20 °C (Ohm/km): 39 ¦ External Diameter (mm): 2,15 ¦ Weight (kg/km): 9 ¦ Class: Eca |
| 1x0,75 | Resistance at 20 °C (Ohm/km): 26 ¦ External Diameter (mm): 2,25 ¦ Weight (kg/km): 11 ¦ Class: Eca |
| 1x1 | Resistance at 20 °C (Ohm/km): 19,5 ¦ External Diameter (mm): 2,50 ¦ Weight (kg/km): 14 ¦ Class: Eca |

ENGINEERING TABLES

H05V-K · Source Specification Table 1

| Section (mm²) | Resistance at 20 °C (Ohm/km) | External Diameter (mm) | Weight (kg/km) | Class |
| --- | --- | --- | --- | --- |
| 1x0,5 | 39 | 2,15 | 9 | Eca |
| 1x0,75 | 26 | 2,25 | 11 | Eca |
| 1x1 | 19,5 | 2,50 | 14 | Eca |

H05V-K · Source Specification Table 2

| 1. Conductor | Flexible electrolytic copper conductor (Class V) according to BS EN 60228:2005 (previously BS6360) and EN 60228. |
| --- | --- |
| 2. Insulation | PVC insulation type TI-1 according to BS7655 and HD 21.3S3:1995/A2:2008. |
| Nominal voltage | 300/500 V |
| Test voltage | 2.000 V A.C. |
| Maximum temperature | 70 °C |
| Other characteristics | — |
| Colours according to HD 21.1S4:2002Non-flame propagating according to UNE-EN 60332-1-2, EN 60332-1-2 and IEC 60332-1-2CPR Classification according to EN 50575 | — |