CABLE & WIRE FOR ELECTRICAL, ELV AND INDUSTRIAL PROJECTS

# H05V-U / H07V-U PVC Insulated Solid Building Wire

Exact model: H05V-U | H07V-U

PRODUCT IMAGES

H05V-U ¦ H07V-U · Primary

PRODUCT OVERVIEW

NexPro H05V-U / H07V-U PVC Insulated Solid Building Wire is supplied as a configurable single-core building wire product family. Catalog models are preserved exactly as H05V-U, H07V-U. Use the source-derived tables below to select the required conductor construction, core arrangement, cross-section and dimensions.

| Product line | Cable & Wire for Electrical, ELV and Industrial Projects |
| --- | --- |
| Series / family | Single-core building wire |
| Exact model | H05V-U ¦ H07V-U |
| Applications | Building wiring, Electrical panels, Fixed installation projects |

MODEL IDENTIFICATION

| Exact model | Product / variant | Cable category | Catalog model | Configuration |
| --- | --- | --- | --- | --- |
| H05V-U ¦ H07V-U | H05V-U / H07V-U PVC Insulated Solid Building Wire | Single-core building wire | H05V-U ¦ H07V-U | Select from source table |

TECHNICAL SPECIFICATIONS

| Parameter | Specification |
| --- | --- |
| Cable category | Single-core building wire |
| Catalog model | H05V-U ¦ H07V-U |
| Configuration | Select from source table |
| Manufacturer models | H05V-U / H07V-U |
| Conductor | Specified value: Bare solid copper |
| Insulation | Specified value: PVC |
| Minimum bending radius, fixed installation | Specified value: 4xOD |
| Colour | Specified value: According to EN 50525-1 |

ENGINEERING TABLES

H05V-U | H07V-U · Construction

| Parameter | Specified value |
| --- | --- |
| Conductor | Bare solid copper |
| Insulation | PVC |
| Minimum bending radius, fixed installation | 4xOD |
| Colour | According to EN 50525-1 |

H05V-U | H07V-U · Source Specification Table 2

| Type Code | Cross-section [mm] | Nominal Outer Diameter [mm] | Current rating, installation in open air, ambient 30°C [A] | Total weight [kg/km] |
| --- | --- | --- | --- | --- |
| H05V-U | 0,5 | 2,0 | 12 | 9 |
| H05V-U | 0,75 | 2,2 | 15 | 11 |
| H05V-U | 1 | 2,3 | 19 | 14 |
| H07V-U | 1,5 | 2,8 | 24 | 20 |
| H07V-U | 2,5 | 3,4 | 32 | 31 |
| H07V-U | 4 | 3,8 | 42 | 46 |
| H07V-U | 6 | 4,3 | 54 | 68 |
| H07V-U | 10 | 5,4 | 73 | 111 |