CABLE & WIRE FOR ELECTRICAL, ELV AND INDUSTRIAL PROJECTS

# Photovoltaic Solar Cable

Exact model: PV Solar Cable

PRODUCT IMAGES

| PV Solar Cable · Primary | PV Solar Cable · Gallery | PV Solar Cable · Gallery |
| --- | --- | --- |

PRODUCT OVERVIEW

NexPro Photovoltaic Solar Cable is supplied as a configurable photovoltaic cable product family. Catalog models are preserved exactly as PV Solar Cable. Use the source-derived tables below to select the required conductor construction, core arrangement, cross-section and dimensions.

| Product line | Cable & Wire for Electrical, ELV and Industrial Projects |
| --- | --- |
| Series / family | Photovoltaic cable |
| Exact model | PV Solar Cable |
| Applications | Solar and utility projects, Outdoor distribution, Project-specific installations |

MODEL IDENTIFICATION

| Exact model | Product / variant | Cable category | Catalog model | Configuration |
| --- | --- | --- | --- | --- |
| PV Solar Cable | Photovoltaic Solar Cable | Photovoltaic cable | PV Solar Cable | Select from source table |

TECHNICAL SPECIFICATIONS

| Parameter | Specification |
| --- | --- |
| Cable category | Photovoltaic cable |
| Catalog model | PV Solar Cable |
| Configuration | Select from source table |
| Manufacturer models | PV Solar Cable |
| 1.5 | Monofilament diameter mm / number of pieces: 0.25/30 ¦ conductor outer diameter mm: 1.6 ¦ Insulation thickness mm: 0.5 ¦ Sheath thickness mm: 0.5 ¦ Finished outer diameter mm: 3.6-4.0 ¦ Approximate weight /km/kg: 32.33 |
| 2.5 | Monofilament diameter mm / number of pieces: 0.25/49 ¦ conductor outer diameter mm: 2.1 ¦ Insulation thickness mm: 0.5 ¦ Sheath thickness mm: 0.5 ¦ Finished outer diameter mm: 4.1-4.4 ¦ Approximate weight /km/kg: 36.82 |
| 4 | Monofilament diameter mm / number of pieces: 0.30/56 ¦ conductor outer diameter mm: 2.6 ¦ Insulation thickness mm: 0.7 ¦ Sheath thickness mm: 0.7 ¦ Finished outer diameter mm: 5.4-5.7 ¦ Approximate weight /km/kg: 67.89 |
| 6 | Monofilament diameter mm / number of pieces: 0.30/84 ¦ conductor outer diameter mm: 3.2 ¦ Insulation thickness mm: 0.7 ¦ Sheath thickness mm: 0.7 ¦ Finished outer diameter mm: 6.5-6.9 ¦ Approximate weight /km/kg: 75.44 |
| 10 | Monofilament diameter mm / number of pieces: 0.40/80 ¦ conductor outer diameter mm: 4.1 ¦ Insulation thickness mm: 0.8 ¦ Sheath thickness mm: 0.7 ¦ Finished outer diameter mm: 7.1-7.5 ¦ Approximate weight /km/kg: 95.64 |
| 16 | Monofilament diameter mm / number of pieces: 0.40/126 ¦ conductor outer diameter mm: 5.2 ¦ Insulation thickness mm: 0.8 ¦ Sheath thickness mm: 0.7 ¦ Finished outer diameter mm: 8.2-8.7 ¦ Approximate weight /km/kg: 110.46 |
| 25 | Monofilament diameter mm / number of pieces: 0.40/196 ¦ conductor outer diameter mm: 6.5 ¦ Insulation thickness mm: 1 ¦ Sheath thickness mm: 0.9 ¦ Finished outer diameter mm: 10.3-10.7 ¦ Approximate weight /km/kg: 175.75 |
| 35 | Monofilament diameter mm / number of pieces: 0.40/276 ¦ conductor outer diameter mm: 7.7 ¦ Insulation thickness mm: 1 ¦ Sheath thickness mm: 0.9 ¦ Finished outer diameter mm: 11.5-12.5 ¦ Approximate weight /km/kg: 196.22 |

ENGINEERING TABLES

PV Solar Cable · Source Specification Table 1

| Cross-sectional area mm² | Monofilament diameter mm / number of pieces | conductor outer diameter mm | Insulation thickness mm | Sheath thickness mm | Finished outer diameter mm | Approximate weight /km/kg |
| --- | --- | --- | --- | --- | --- | --- |
| 1.5 | 0.25/30 | 1.6 | 0.5 | 0.5 | 3.6-4.0 | 32.33 |
| 2.5 | 0.25/49 | 2.1 | 0.5 | 0.5 | 4.1-4.4 | 36.82 |
| 4 | 0.30/56 | 2.6 | 0.7 | 0.7 | 5.4-5.7 | 67.89 |
| 6 | 0.30/84 | 3.2 | 0.7 | 0.7 | 6.5-6.9 | 75.44 |
| 10 | 0.40/80 | 4.1 | 0.8 | 0.7 | 7.1-7.5 | 95.64 |
| 16 | 0.40/126 | 5.2 | 0.8 | 0.7 | 8.2-8.7 | 110.46 |
| 25 | 0.40/196 | 6.5 | 1 | 0.9 | 10.3-10.7 | 175.75 |
| 35 | 0.40/276 | 7.7 | 1 | 0.9 | 11.5-12.5 | 196.22 |