CABLE & WIRE FOR ELECTRICAL, ELV AND INDUSTRIAL PROJECTS

# H03VV-F Light Duty PVC Flexible Cord

Models: H03VV-F | H05VV-F | 60227 IEC 53 (RVV) | RVV

PRODUCT IMAGES

| H03VV-F · Primary | H05VV-F · Primary | H05VV-F · Gallery | H05VV-F · Gallery |
| --- | --- | --- | --- |

| H05VV-F · Gallery | 60227 IEC 53 (RVV) ¦ RVV · Primary |
| --- | --- |

PRODUCT OVERVIEW

NexPro H03VV-F Light Duty PVC Flexible Cord is supplied as a configurable pvc flexible cord product family. Catalog models are preserved exactly as H03VV-F. Use the source-derived tables below to select the required conductor construction, core arrangement, cross-section and dimensions.

| Product line | Cable & Wire for Electrical, ELV and Industrial Projects |
| --- | --- |
| Series / family | PVC flexible cord |
| Exact model | H03VV-F ¦ H05VV-F ¦ 60227 IEC 53 (RVV) ¦ RVV |
| Applications | Equipment connections, Flexible wiring, OEM electrical assemblies |

MODEL COMPARISON

| Exact model | Product / variant | Cable category | Catalog model | Configuration |
| --- | --- | --- | --- | --- |
| H03VV-F | H03VV-F Light Duty PVC Flexible Cord | PVC flexible cord | H03VV-F | Select from source table |
| H05VV-F | H05VV-F Ordinary Duty PVC Flexible Cable | PVC flexible cord | H05VV-F | Select from source table |
| 60227 IEC 53 (RVV) ¦ RVV | RVV PVC Insulated Flexible Sheathed Cable | PVC flexible cord | 60227 IEC 53 (RVV) ¦ RVV | Select from source table |

TECHNICAL SPECIFICATIONS

| Parameter | H03VV-F | H05VV-F | 60227 IEC 53 (RVV) ¦ RVV |
| --- | --- | --- | --- |
| Cable category | PVC flexible cord | PVC flexible cord | PVC flexible cord |
| Catalog model | H03VV-F | H05VV-F | 60227 IEC 53 (RVV) ¦ RVV |
| Configuration | Select from source table | Select from source table | Select from source table |
| Manufacturer models | H03VV-F | H05VV-F | 60227 IEC 53 (RVV) / RVV |
| 2x0,5 | Resistance at 20 °C (Ohm/km): 39 ¦ External Diameter (mm): 4,75 ¦ Weight (kg/km): 40 ¦ Class: Eca | Not provided | Not provided |
| 2x0,75 | Resistance at 20 °C (Ohm/km): 26 ¦ External Diameter (mm): 5,20 ¦ Weight (kg/km): 41 ¦ Class: Eca | Not provided | Not provided |
| 3G0,5 | Resistance at 20 °C (Ohm/km): 39 ¦ External Diameter (mm): 5,25 ¦ Weight (kg/km): 42 ¦ Class: Eca | Not provided | Not provided |
| 3G0,75 | Resistance at 20 °C (Ohm/km): 26 ¦ External Diameter (mm): 5,50 ¦ Weight (kg/km): 49 ¦ Class: Eca | Not provided | Not provided |
| 4x0,5 | Resistance at 20 °C (Ohm/km): 39 ¦ External Diameter (mm): 5,60 ¦ Weight (kg/km): 47 ¦ Class: Eca | Not provided | Not provided |
| 4x0,75 | Resistance at 20 °C (Ohm/km): 26 ¦ External Diameter (mm): 6,30 ¦ Weight (kg/km): 64 ¦ Class: Eca | Not provided | Not provided |
| Specification status | Not provided | No numeric source table was published for this product family | No numeric source table was published for this product family |
| Selection guidance | Not provided | Confirm the exact model, voltage rating, conductor or core configuration, cross-section, installation conditions, required length and applicable project requirements in the RFQ. | Confirm the exact model, voltage rating, conductor or core configuration, cross-section, installation conditions, required length and applicable project requirements in the RFQ. |

ENGINEERING TABLES

H03VV-F · Source Specification Table 1

| Section (mm²) | Resistance at 20 °C (Ohm/km) | External Diameter (mm) | Weight (kg/km) | Class |
| --- | --- | --- | --- | --- |
| 2x0,5 | 39 | 4,75 | 40 | Eca |
| 2x0,75 | 26 | 5,20 | 41 | Eca |
| 3G0,5 | 39 | 5,25 | 42 | Eca |
| 3G0,75 | 26 | 5,50 | 49 | Eca |
| 4x0,5 | 39 | 5,60 | 47 | Eca |
| 4x0,75 | 26 | 6,30 | 64 | Eca |

H03VV-F · Source Specification Table 2

| 1. Conductor | Flexible electrolytic copper conductor (Class V) according to BS EN 60228:2005 (previously BS6360) and UNE 60228. |
| --- | --- |
| 2. Insulation | PVC insulation type TI-2 according to BS7655, UNE-EN 50363-3 and EN 50363-3 |
| 3. Sheath | PVC sheath type TM-2 according to BS7655, UNE-EN 50363-4-1 and EN 50363-4-1 |
| Nominal voltage | 300/300 V |
| Test voltage | 2.000 V A.C. |
| Maximum temperature | 70 °C |
| Other characteristics | — |
| Colours according to UNE 21089 and HD 303S2 (colour marking when less than five conductors) and UNE-EN 50334 and EN 50334 (inscription marking when more than five conductors)Non-flame propagating according to UNE-EN 60332-1-2, EN 60332-1-2 and IEC 60332-1-2PVC with reduced hydrogen chloride (HCI) emissionCPR Classification according to EN 50575 | — |