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CABLE & WIRE FOR ELECTRICAL, ELV AND INDUSTRIAL PROJECTS
Photovoltaic Solar Cable
Exact model: PV Solar Cable
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PRODUCT OVERVIEW
NexPro Photovoltaic Solar Cable is supplied as a configurable photovoltaic cable product family. Catalog models are preserved exactly as PV Solar Cable. Use the source-derived tables below to select the required conductor construction, core arrangement, cross-section and dimensions.
	Product line
	Cable & Wire for Electrical, ELV and Industrial Projects

	Series / family
	Photovoltaic cable

	Exact model
	PV Solar Cable

	Applications
	Solar and utility projects, Outdoor distribution, Project-specific installations


MODEL IDENTIFICATION
	Exact model
	Product / variant
	Cable category
	Catalog model
	Configuration

	PV Solar Cable
	Photovoltaic Solar Cable
	Photovoltaic cable
	PV Solar Cable
	Select from source table


TECHNICAL SPECIFICATIONS
	Parameter
	Specification

	Cable category
	Photovoltaic cable

	Catalog model
	PV Solar Cable

	Configuration
	Select from source table

	Manufacturer models
	PV Solar Cable

	1.5
	Monofilament diameter mm / number of pieces: 0.25/30 | conductor outer diameter mm: 1.6 | Insulation thickness mm: 0.5 | Sheath thickness mm: 0.5 | Finished outer diameter mm: 3.6-4.0 | Approximate weight /km/kg: 32.33

	2.5
	Monofilament diameter mm / number of pieces: 0.25/49 | conductor outer diameter mm: 2.1 | Insulation thickness mm: 0.5 | Sheath thickness mm: 0.5 | Finished outer diameter mm: 4.1-4.4 | Approximate weight /km/kg: 36.82

	4
	Monofilament diameter mm / number of pieces: 0.30/56 | conductor outer diameter mm: 2.6 | Insulation thickness mm: 0.7 | Sheath thickness mm: 0.7 | Finished outer diameter mm: 5.4-5.7 | Approximate weight /km/kg: 67.89

	6
	Monofilament diameter mm / number of pieces: 0.30/84 | conductor outer diameter mm: 3.2 | Insulation thickness mm: 0.7 | Sheath thickness mm: 0.7 | Finished outer diameter mm: 6.5-6.9 | Approximate weight /km/kg: 75.44

	10
	Monofilament diameter mm / number of pieces: 0.40/80 | conductor outer diameter mm: 4.1 | Insulation thickness mm: 0.8 | Sheath thickness mm: 0.7 | Finished outer diameter mm: 7.1-7.5 | Approximate weight /km/kg: 95.64

	16
	Monofilament diameter mm / number of pieces: 0.40/126 | conductor outer diameter mm: 5.2 | Insulation thickness mm: 0.8 | Sheath thickness mm: 0.7 | Finished outer diameter mm: 8.2-8.7 | Approximate weight /km/kg: 110.46

	25
	Monofilament diameter mm / number of pieces: 0.40/196 | conductor outer diameter mm: 6.5 | Insulation thickness mm: 1 | Sheath thickness mm: 0.9 | Finished outer diameter mm: 10.3-10.7 | Approximate weight /km/kg: 175.75

	35
	Monofilament diameter mm / number of pieces: 0.40/276 | conductor outer diameter mm: 7.7 | Insulation thickness mm: 1 | Sheath thickness mm: 0.9 | Finished outer diameter mm: 11.5-12.5 | Approximate weight /km/kg: 196.22


ENGINEERING TABLES
PV Solar Cable · Source Specification Table 1
	Cross-sectional area mm²
	Monofilament diameter mm / number of pieces
	conductor outer diameter mm
	Insulation thickness mm
	Sheath thickness mm
	Finished outer diameter mm
	Approximate weight /km/kg

	1.5
	0.25/30
	1.6
	0.5
	0.5
	3.6-4.0
	32.33

	2.5
	0.25/49
	2.1
	0.5
	0.5
	4.1-4.4
	36.82

	4
	0.30/56
	2.6
	0.7
	0.7
	5.4-5.7
	67.89

	6
	0.30/84
	3.2
	0.7
	0.7
	6.5-6.9
	75.44

	10
	0.40/80
	4.1
	0.8
	0.7
	7.1-7.5
	95.64

	16
	0.40/126
	5.2
	0.8
	0.7
	8.2-8.7
	110.46

	25
	0.40/196
	6.5
	1
	0.9
	10.3-10.7
	175.75

	35
	0.40/276
	7.7
	1
	0.9
	11.5-12.5
	196.22
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